产品规格书

# 5050RGB

Outline Dimension:

- View Angle:

Absolute Maximum Ratings (Ta = 25℃)

| Items项目 | Symbol符号 | Absolute maximum Rating | Unit |
| --- | --- | --- | --- |
| Power Dissipation | PD | 200 | mW |
| Forward Current(DC) | IF | 60 | mA |
| Peak Forward Current | IFP | 100 | mA |
| Reverse Voltage | VR | 5 | V |
| Operation Temperature | Topr | ﹣20～﹢85 | ℃ |
| Storage Temperature | Tstg | ﹣30～﹢80 | ℃ |
| Lead Soldering Temperature | Tsol | Max.260℃ for 5 sec Max. (3min from the base of the epoxy bulb) |  |

Pulse width≤0.1msec duty≤1/10

Typical Electrical & Optical Characteristics(Ta=25°)

| Items | Symbol | Condition | Min | Typ | Max | Unit |
| --- | --- | --- | --- | --- | --- | --- |
| Forward Voltage | VF | IF =60mA | R：2.0 G：3.0 B：3.0 | --- | R：2.2 G：3.3 B：3.3 | V |
| Reverse Current | IR | VR =5V | --- | --- | 10 | μA |
| Chromatic Coordinates | X,Y | IF =60mA | --- | --- | --- |  |
| Luminous Intensity | Iv | IF =60mA*3 | R：1800 G：2700 B：1200 | --- | R：2000 G：3000 B：1500 | mcd |
| View Angle | 2θ1/2 | IF =60mA | --- | 150 | --- | Deg |
| Dominant Wavelength | WD | IF =60mA | R:620 G:520 B:465 | --- | R:630 G:530 B:470 | nm |

可根据客户要求订做特殊规格产品